SECTION 03 49 00

CASTWORKS GLASS FIBER REINFORCED CONCRETE (GFRC) ARCHITECTURAL FORMS

Part 1 – GENERAL

1.1	RELATED DOCUMENTS

This specification is general outline of the CastWorks Glass Fiber Reinforced Concrete (GFRC) requirements, as they pertain to the overall project design. In all cases, the Manufacturer’s printed specifications shall govern the work of this section.

1.2	SUMMARY

- Section Includes:

  - Furnish all materials, labor, equipment, and services necessary for the supply and installation of CastWorks GFRC components as indicated on the drawings and contract documents.

  - Work shall include supply of GFRC components, installation, patching, repairing, and cleaning.

- Related Sections:

  - Section 03 49 13 Glass-Fiber Reinforced Column Covers

  - Section 03 49 43 Glass Fiber Reinforced Concrete Trim

  - Section 05 10 00 Structural Metal Framing

  - Section 05 40 00 Cold-Formed Metal Framing

  - Section 06 10 00 Rough Carpentry

  - Section 07 90 00 Joint Protection

  - Section 09 29 00 Gypsum Board

  - Section 09 90 00 Painting and Coating

- Substitutions:

  - Manufacturers desiring to submit proposals other than CastWorks GFRC shall, at least 10 days prior to the bid date, submit to the Architect all descriptive information of the system. These Manufacturers must have a minimum of three years’ experience with the system, provide photographs, and shop drawings of at least three projects similar in detail and scope with names, addresses and phone contacts of the respective Architects and Installation Contractors. Independent test data showing compliance with the specified system and three samples of similar details must also be submitted.

1.3	References

- American Society for Testing and Materials (ASTM):

  - ASTM D638 Standard Test Method for Tensile Properties of Plastics

  - ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials

  - ASTM C109/C109M Standard Test Method for Compressive Strength of Hydraulic Cement Mortars (Using 2-in. or [50-mm] Cube Specimens)

  - ASTM C947 Standard Test Method for Flexural Properties of Thin-Section Glass-Fiber-Reinforced Concrete (Using Simple Beam with Third-Point Loading)

  - ASTM D256 Standard Test Methods for Determining the Izod Pendulum Impact Resistance of Plastics

  - ASTM D696 Standard Test Method for Coefficient of Linear Thermal Expansion of Plastics Between −30°C and 30°C with a Vitreous Silica Dilatometer

  - ASTM C473 Standard Test Methods for Physical Testing of Gypsum Panel Products

  - ASTM C177 Standard Test Method for Steady-State Heat Flux Measurements and Thermal Transmission Properties by Means of the Guarded-Hot-Plate Apparatus

  - ASTM E136 Standard Test Method for Behavior of Materials in a Vertical Tube Furnace at 750°C

  - ASTM G23 Standard Practice for Operating Light-Exposure Apparatus (Carbon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials

1.4	SUBMITTALS

- Submit a minimum of three 3" x 3" or 8" x 8" CastWorks GFRC flat samples to the Architect for his review.

- Submit shop drawings for approval showing plans, sections, details, joint treatment, reinforcing, fastening devices and the relation of the GFRC components to the surrounding construction.

- Product Data: Submit manufacturer’s technical data.

1.5	RESPONSIBILITY

- The Installation Contractor shall install and work under this section and he will be responsible for coordinating the installation with other trades.

1.6	MOCK-UP

- Prior to production, erect one proto-type component on-site or at the Armstrong CastWorks plant, for review by the Architect.

1.7	DELIVERY, STORAGE, HANDLING AND PROTECTION

- Transport and handle units in a manner that avoids excessive stresses or damage.

- Components displaying obvious damage must be rejected at site at time of delivery.

- Store the components in a weather protected environment, on level surfaces, with temporary supports as required. Do not stack or lean.

1.8	Warranty

One year from substantial completion.

PART 2. – PRODUCTS

2.1	MANUFACTURER

- CastWorks by Armstrong World Industries, Inc.

2.2	MATERIALS

- CastWorks GFRC components shall be asbestos free and prefabricated with portland cement, polymers, aggregates, and reinforced with chopped strand fibers.

- CastWorks GFRC components shall be suitably reinforced with steel.

- Fabrication will be as per approved shop drawings and will not include framing or assembly. If multiple components are required to complete design criteria as per contract drawings, additional site work under related sections, installation or finishing may be required.

- Finishes:

  - Smooth, paint grade (field priming and painting required by others) see project painting specification.

  - Sandblast texture, integrally colored in one of CastWorks GFRC 12 standard colors.

  - Sandblast texture, integrally colored in a custom color.

2.3		TOLERANCES (FABRICATION)

- Dimensional - all directions +/- 1/8"

- Thickness - skin +/- 1/8"

- Warpage or Bowing +/- 1/16"/foot

- Site conditions and normal manufacturing variations may require additional site work to maintain these tolerances.

2.4	PHYSICAL PROPERTIES

- Shell Thickness ½"

- Weight (depending on shape and reinforcement) 4 - 7 lbs/sq.ft

- Density 130 - 140 lbs/cu.ft

- Compressive Strength (ASTM C-109-92 Mod.) 9,810 psi.

- Flexural Strength (ASTM C-947-89 Mod.) 2,562 psi.

- Modulus of Elasticity - In Flexure (ASTM D638) 2.28 x 106 psi.

- Tensile Strength (ASTM D-638) 940 psi.

- Impact Strength (ASTM D-256-93a; Notched) 1.30 ft-lbs/in of notch

- Coefficient of Linear Thermal Expansion (ASTM D-696) 0.60 x 10-5/˚F

- Humidified Deflection (ASTM C-473-95) No Measurable Value

- Thermal Conductivity (ASTM C-177-85) 4.35 Btu-in/hr-ft2-˚F

- Fuel Contribution (ASTM E-136-98a) Complied with requirements

- Flame Spread (ASTM E-84-98) 0, Class A

- Smoke Index (ASTM E-84-98) 0, Class A

- Resistance to Weathering (ASTM G-23-93) Class 5, Negligible color alteration

- Screw Withdrawal (standard lab procedure) 346 lbs

- Fiber Content 4% - 6% by weight

  - INSPECTION

- The Architect or his representative shall have access to the manufacturing facilities, either prior to contract award or thereafter, to inspect or verify compliance with the above specifications.

3.0	EXECUTION

3.1	PRE-INSTALLATION RESPONSIBILITY

- Field Measurements: Prior to manufacturing, the Installer will be responsible for obtaining all field dimensions for inclusion on the Manufacturer’s shop drawings.

- Coordination: The Installer will be responsible for the co-ordination of the installation with related sections, within the tolerances specified in the respective articles.

- Discrepancies: Prior to installation, the Installer shall check job site dimensions and conditions. Any discrepancies between design and field dimensions shall be brought to the attention of the General Contractor and the Architect.

3.2	INSTALLATION

- Components shall be lifted/handled with suitable devices.

- Handle units with clean gloves.

- Components shall be installed plum and true. Shim where necessary.

- Pre-drill and countersink to 1/8" minimum below finished surface of unit if required.

- Fasten components with stainless steel fasteners through embedded steel or face of GFRC as indicated on shop drawings.

- Use PL Premium construction adhesive where indicated on shop drawings.

- Where components are suspended, use as a minimum 12 gauge galvanized steel wire and the suspension points indicated on the shop drawings.

- Framing, hangers, etc., as specified elsewhere.

- Joints are to be caulked as specified under Sealants and Caulking.

3.3	PATCHING AND CONTROL JOINTS

- Introduce control joints as required (35'-0" O.C.) under related section of the Specification.

- Patch any damage to match component texture, using mix and sealer provided by CastWorks or Installer. Contact CastWorks at 1.800.268.4534 and speak to a qualified technician before patching GFRC.

  - CLEANING

- For painted GFRC, refer to paint specification.

- For integrally colored GFRC, use a liquid soap and warm water solution for mild stains. For tougher stains, use a light duty concrete cleaner. Call Castworks on 1-800-268-4534 and speak with a technical representative before cleaning GFRC.

  - NOTES

- CastWorks GFRC components shall be used for Interior or Exterior Applications.

- GFRC may exhibit imperfections. To achieve satisfactory results, additional finishing may be required.