SECTION 06 60 00

CASTWORKS™ GLASS FIBER REINFORCED POLYESTER RESIN (FRP) 
ARCHITECTURAL FORMS

Part 1 – GENERAL

1.1 RELATED DOCUMENTS

This specification is a general outline of the CastWorks FRP requirements, as they pertain to the overall project design. In all cases, the Manufacturer’s printed specifications shall govern the work of this section.

1.2 SUMMARY

- Section Includes:

  - Furnish all materials, labor, equipment, and services necessary for the supply and installation of CastWorks FRP components as indicated on the drawings and contract documents.

  - Work shall include supply of FRP components, installation, and joint treatment.

- Related Sections:

  - Section 05 10 00 Structural Metal Framing

  - Section 06 10 00 Rough Carpentry

  - Section 07 90 00 Joint Protection

  - Section 09 29 00 Gypsum Board

  - Section 09 90 00 Painting and Coating

- Substitutions:

  - Manufacturers desiring to submit proposals other than CastWorks FRP shall, at least 10 days prior to the bid date, submit to the Architect all descriptive information of the system. These Manufacturers must have a minimum of five years’ experience in architectural fiberglass reinforced fabrications. Independent test data showing compliance with the specified system and three samples of similar details must also be submitted.

1.3 References

- American Society for Testing and Materials (ASTM):

  - ASTM D790 Standard Test Methods for Flexural Properties of Unreinforced and Reinforced Plastics and Electrical Insulating Materials

  - ASTM D638 Standard Test Method for Tensile Properties of Plastics

  - ASTM D2583 Standard Test Method for Indentation Hardness of Rigid Plastics by Means of a Barcol Impressor

  - ASTM D695 Standard Test Method for Compressive Properties of Rigid Plastics

  - ASTM D570 Standard Test Method for Water Absorption of Plastics

  - ASTM E84 Standard Test Method for Surface Burning Characteristics of Building Materials

1.4   SUBMITTALS

- Submit a minimum of three 3" x 3" or 8" x 8" CastWorks FRP samples illustrating color, texture and finish.

- Submit shop drawings for approval showing plans, sections, details, joint treatment, reinforcing, fastening devices and the relation of the CastWorks FRP components to the surrounding construction.

- Product Data: Submit manufacturer’s technical data.

1.5	RESPONSIBILITY

- The Installation Contractor shall install and work under this section and he will be responsible for coordinating the installation with other trades.

1.6	MOCK-UP

- Prior to production, erect one proto-type on-site or at the Armstrong CastWorks plant, for review by the Architect.

1.7   DELIVERY, STORAGE, HANDLING AND PROTECTION

- Transport and handle units in a manner that avoids excessive stresses or damage.

- Components displaying obvious damage must be rejected at site at time of delivery.

- Store the components in a weather protected environment, on level surfaces, with temporary supports as required. Do not stack or lean.

1.8   Warranty

One year from substantial completion.

PART 2. – PRODUCTS

2.1	MANUFACTURER

- CastWorks by Armstrong World Industries, Inc.

2.2	MATERIALS

- Gelcoat: 18 mils thick, UV resistant

- Glass: E Glass Fiber. Glass Content 20 - 32%.

- Laminate: Nominal thickness 3/16". Additional thickness and reinforcing as indicated or required for structural integrity.

- Finishes:

  - Unfinished sanding gelcoat. Field priming and painting required.

  - Pre-finished gelcoat.

  - Factory applied urethane.

  - Simulated stone.

2.3	TOLERANCES (FABRICATION)

- Dimensional – all directions +/- 1/8"

- Thickness – skin +/- 1/16"

- Warpage or Bowing +/- 1/16"/foot

- Gelcoat Thickness	+/- 5.0 mils

- Site conditions and normal manufacturing variations may require additional site work to maintain these tolerances.

2.4	PHYSICAL PROPERTIES

- Flame Spread (ASTM E84) Class A

- Flexural Strength (ASTM D790) 19600 psi.

- Flexural Modulus (ASTM D790) 16 x 105 psi.

- Tensile Strength (ASTM D638) 11300 psi.

- Tensile Elongation (ASTM D638) 1.75%

- Barcol Hardness (ASTM D2583) 67–75

- Compressive Strength (ASTM D695) 22200 psi.

- Water Absorption (ASTM D570) 0.06

- Izod Impact Strength (ASTM D-256 Notched) 12.6 ft. lbs/inch of notch

  - INSPECTION

- The Architect or representative shall have access to the manufacturing facilities, either prior to contract award or thereafter, to inspect or verify compliance with the above specifications.

3.0	EXECUTION

3.1	PRE-INSTALLATION RESPONSIBILITY

- Field Measurements: Prior to manufacturing, the Installer will be responsible for obtaining all field dimensions for inclusion on the Manufacturer’s shop drawings.

- Coordination: The Installer will be responsible for the co-ordination of the installation with related sections, within the tolerances specified in the respective articles.

- Discrepancies: Prior to installation, the Installer shall check job site dimensions and conditions. Any discrepancies between design and field dimensions shall be brought to the attention of the General Contractor and the Architect.

3.2	INSTALLATION

- Components shall be installed in accordance with architectural drawings, approved shop drawings and Manufacturer’s instructions.

3.3 	CLEANING

- Clean components in accordance with Manufacturer’s instructions.

- Clean soiled FRP units with mild detergent and clean water using a soft cloth. Rinse thoroughly with clean water.

- For pre-finished FRP, contact CastWorks at 1-800-268-4534 and speak with a qualified technician before cleaning.

- For unfinished FRP, refer to paint specification.

3.4	NOTES

- CastWorks FRP components shall be used for Interior or Exterior Applications.

- CastWorks FRP can experience slight variation in color, texture and thickness.