Lamit Industries, Inc.

710 Marion Road

Columbus, Ohio 43207

P-(614)444-3010

F-(614)444-4264

info@lamitindustries.com

www.lamitindustries.com

SECTION 07 22 16

NailBase InsulatioN

GENERAL

SUMMARY

Section Includes: Nailbase Insulation.

Related Sections: Section(s) related to this section include:

Section 06 10 00 Rough Carpentry

SYSTEM DESCRIPTION

    - Nailbase Insulation consisting of oriented strand board (OSB) laminated to an expanded polystyrene (EPS) insulation core.

REFERENCES

ASTM C578 – Standard Specification for Rigid, Cellular Polystyrene Thermal Insulation.

PS2 - Performance Standard for Wood-based Structural-use Panels.

ICC ES AC12 – Acceptance Criteria for Foam Plastic Insulation.

SUBMITTALS

Product Data: Submit product data for specified products.

EPS Code Compliance: Provide ICC ES code report for EPS foam with evidence of compliance with code. Code report shall include compliance with ICC ES AC12 (Foam Plastic) and dated July 2009.

Manufacturer’s Instructions:  Nailbase Insulation manufacturer’s installation guidelines.

Quality Assurance Submittals: Submit the following:

Certificate: certificate showing compliance of EPS insulation to Third Party Quality Control program of Underwriters Laboratories, Inc.

Warranty:  Warranty documents specified herein.

QUALITY ASSURANCE

Source Limitations:  Obtain all Nailbase Insulation through one source.  All accessories to be as furnished or recommended by the Nailbase Insulation manufacturer.

DELIVERY, STORAGE & HANDLING

Delivery: Deliver materials from Nailbase Insulation manufacturer with identification labels or markings intact.

Storage:  Store products off the ground, in dry conditions, under cover until ready for installation. Protect insulation from open flame and keep dry at all times.

PRODUCTS

Manufacturers/Suppliers:

    - Lamit Industries, Inc. 710 Marion Rd., Columbus, OH 43207 www.lamitindustries.com Phone 614-444-3010

Materials

Nailbase Insulation consisting of the following:

UL certified EPS core complying with ASTM C578 Type I insulation.  Insulation manufacturer shall provide Third Party UL certificate.

OSB identified with APA or PFS performance mark with Exposure I durability rating and performance in accordance with DOC PS-2 span rating 24/16 or greater.

Accessories

Fasteners:  corrosion resistant SIP screws compatible with the Nailbase Insulation shall be provided by the Nailbase Insulation manufacturer.

      - Wood Screws for attachment to wood members

      - Heavy Duty Metal Screws for attachment to metal members (16 gauge to 3/16”)

      - Light Duty Metal Screws for attachment to metal decks (18 gauge or thinner)

Splines: As required, OSB splines shall be supplied by the Nailbase Insulation manufacturer.

Sealant:  As required, Sealant shall be specifically designed for use with Nailbase Insulation.  Sealant shall be provided by the Nailbase Insulation manufacturer.

Dimensional Lumber:  SPF, #2 or better, or engineered equivalent unless otherwise required by architectural drawings.

Insulation Size

Sizes:  Nailbase Insulation shall be manufactured to sizes in accordance with the approved architectural drawings

Thermal Resistance, R-value

1.	      4” thick (Nom.) Nailbase Insulation with R-value of 15 at 75oF (16 at 40oF)

2.	      6” thick (Nom.) Nailbase Insulation with R-value of 23 at 75oF (24 at 40oF)

      - 8” thick (Nom.) Nailbase Insulation with R-value of 30 at 75oF (32 at 40oF)

      - 10” thick (Nom.) Nailbase Insulation with R-value of 38 at 75oF (40 at 40oF)

      - 12“  thick (Nom.) Nailbase Insulation with R-value of 46 at 75oF (48 at 40oF)

PRODUCT SUBSTITUTIONS

Substitutions: No substitutions permitted without thirty day (30) prior approval.

SOURCE QUALITY

Source Quality Assurance: All components (excluding dimensional lumber) required shall be supplied by Nailbase Insulation manufacturer or its approved supplier.

1.	Provide evidence of UL Third Party inspection and labeling of all EPS insulation used in manufacture of Nailbase Insulation.

2. 	Nailbase Insulation manufacturer shall provide 20 year 100% R-Value warranty.

Source Quality: Obtain Nailbase Insulation from a single manufacturer.

EXECUTION

MANUFACTURER’S INSTRUCTIONS

Compliance: Install in accordance with manufacturer's instructions.

Deviations from standard detail and design values shall be approved by the architect/engineer for the project.

EXAMINATION

Site Verification of Conditions: Verify substrate conditions (which have been previously installed under other sections) are acceptable for product installation in accordance with manufacturer’s instructions.

INSTALLATION

Nailbase Insulation Installation:

      - Fastening: Attach Nailbase Insulation with OSB facing up, to structural deck/substrate, using SIP screws as shown on drawings. SIP screw to have a minimum of 1" (25.4 mm) penetration into structural deck/substrate.

Vapor Retarders: Provide vapor retarders as mandated by building code or engineering analysis.

PROTECTION

Protection: Protect installed product and finish surfaces from damage during construction.

Protect Nailbase Insulation from weather by installing roofing materials to provide temporary protection at the end of the day or when rain or snow is imminent.

Install weather resistant roofing and/or cladding materials per roofing and/or cladding manufacturers’ specifications and recommendations.

Nailbase Insulation shall be protected from exposure to solvents and their vapors.

END OF SECTION